## Slide 1
2019
Benefits of
implementing
nickel tablets
TECHNODEL

## Slide 2: Implementing nickel in HDG (1)
Significant growth in producing high silicon steels since 1980’s, had resulted in increasing interest of implementing nickel in hot dip galvanizing.
Production of high silicon steel in the world
year
Japan
France
Italy
Belgium
G.Britain
USA
Luxemburg
F. USSR
Germany

## Slide 3: Implementing nickel in HDG (2)
Increasing implementing nickel in HDG resulted in substantial reduction of zinc consumption per a ton of galvanized steel.
Share of steel galvanized with nickel, %
Zinc consumption, kg/t
Years
Tendency of nickel implementing and zinc consumption in HDG

## Slide 4: Benefits of applying nickel to zinc alloy
Applying nickel to a hot zinc alloy allows to reduce zinc coating thickness, which is especially meaningful in case of reactive steel grades.
Reducing a thickness of zinc coating will improve zinc consumption efficiency, at the rate of 5% to 20% per month (depending on steel items parameters and technology level at HDG plant)
Illustration:
For HDG plant consuming 150 ton of zinc, an economy of 5 % in zinc consumption means saving of 15,000 USD*
*(1t Zn = 2K$)
Sandeline Curve

## Slide 5: Nickel applying methods
3 methods of applying nickel into hot zinc alloy:
  Zinc-nickel alloy
  Nickel powder injection into the zinc kettle
  Nickel tablets

## Slide 6: Zinc-Nickel Alloy
Zinc-nickel alloy blocks (ingots) inserted into the bath, together with blocks of zinc.

## Slide 7: Ni Injection
Alloying a bath with nickel powder is employing special equipment and machinery, such as injection tube operated with inert gas, and a crane.
It’s practically impossible to control exact amount of nickel powder at a specific zone of a bath, therefore a possibility of high local concentration of nickel can’t be excluded.

## Slide 8: Nickel Tablets
Tablets applied by a worker straightly to the bath surface.
The whole operation till the nickel dissolves takes overall below 30 minutes, and afterward galvanizing process could be restarted.
An ability to distribute tablets equally on the bath surface reduces the risk of high nickel concentration zones and therefore the nickel loss to dross.

## Slide 9: Zinc-Nickel alloying - key parameters
An amount of nickel added to a zinc bath for sustaining the Ni concentration level
Time period of initial charging a zinc bath with nickel
Simplicity of alloying process, necessity of special equipment or machinery
Ability to control a nickel concentration level at local zones of a bath, where the alloy is applied
Monthly spending of the HDG plant on nickel alloy

## Slide 10: Zinc-nickel alloying methods - comparative analysis
Zinc-nickel alloy
Nickel tablets
Nickel injection
0.9-1.5 kg | 1.7-1.9 kg | 1.7 kg | Nickel amount (per ton of Zn, for 0.05%)
Up to 2 days | Up to 2 days | Weeks | Initial charging
Very simple | High complexity | Medium complexity | Process simplicity, machinery
Very high | Medium | Low | Nickel concentration control flexibility
Low | Medium | High | Monthly spending on nickel

## Slide 11: Nickel loss during bath alloying operation (1)
Zinc-nickel master alloy:
  high local concentration of nickel
  presence of hard dissolving zinc-nickel intermetallide at the alloy
  reducing zinc temperature at the zone of master alloy local dissolving
Nickel powder:
  practically impossible to control a local nickel concentration at the zone of injection
  partial loss of nickel powder due to hard dissolving “oxidation skin” (usually a commercial nickel powder contain up to 8% of oxygen)

## Slide 12: Nickel loss during bath alloying operation (2)
Nickel tablets Technodel - almost 100% dissolving nickel:
  chemical components in tablet dissolve the “oxidation skin” of nickel powder
  chemical components in tablet reduce a surface strange of zinc in the bath
  fully controlled local nickel concentration at the dissolving zone
  the whole depth of zinc bath is involved for nickel dissolving
Lost Nickel is found at dross:
Master alloy ZnNi0.5% – nickel content 0.4-1%
Nickel tablet Technodel – nickel content 0.2-0.25%

## Slide 13: Nickel consumption during the galvanizing process
Nickel consumption during the galvanizing process doesn’t depend on an alloying method.
Reasons for nickel concentration decrease at zinc bath:
  Adding new zinc to the bath
  Consumption as a part of coating
  Loss to dross

## Slide 14: Nickel consumption as a part of coating
Average nickel concentration at coating depends on a type of steel and always higher than nickel concentration at the zinc bath.
Higher levels of silicon in steel reflect in higher mass of nickel in the coating.
Distribution of elements through zinc coating phases
Si=0.085%
Si=0.227%
Si=0.028%
Element concentration, %
Coating phase, mkm
Element concentration, %
Coating phase, mkm
Element concentration, %
Coating phase, mkm
Si=0.767%
Element concentration, %
Coating phase, mkm

## Slide 15: Loss of nickel to dross during period of galvanizing
Loss of nickel to dross depends on:
  Average temperature of zinc at the bath
  Fe concentration at the zinc
Amount of Fe inserted to bath depends on:
  Pickling process
  Number of rinsing bathes
  Amount of Fe++ in flux
  Temperature at Dryer furnace
Dissolving of Fe in Zn and Zn-Ni